*) MULTIPAIR AES/EBU DMX & POWER COMBI CABLE

1. 개요

본 제품은 멀티 콤비 케이블로 다음과 같은 규격에 준한다.

2. 기능 및 특성

전원선과 DMX 신호를 하나의 케이블에 사용하여 조명기기의 병행 컨트롤

면과 비스코스로 만들어진 원형의 외피로 인해 매우 유연하고 내구성이 강함

촘촘한 나선형의 구리 메쉬 스크린과 꼬은 형태의 동으로 인해 DMX 라인과 한 쌍의 아주 좋은 차폐 효과

적용: DMX 조명 콘솔을 위한 컨트롤 선(웨이브 임피던스 110Ω), 전원 공급과 함께 아날로그 디지털 오디오 멀티채널 제공 등

3. 규격 및 사양

Properties	: OFC oxygen free copper

Signal transmission	: symmetrical

Construction	: [3LIY1,5mm²+ 1x(2LI2Y0,14mm²)DY]VLY

Construction (power)	: 3LIY1,5mm²

Construction (AES/EBU, DMX)	: 1x(2LI2Y0.14mm²)DY

Jacket material	: PVC

Jacket Ø [mm]	: 9,50

Jacket Ø (power) [mm]	: 0,00

Jacket Ø (AES/EBU, DMX) [mm]	: 3,00

Number of Channels (power)	: 1

Number of Channels (AES/EBU, DMX)	: 1

Inner conductor (power)	: 3

Inner conductor (AES/EBU, DMX)	: 2

Inner conductor (power) [mm²]	: 1,50

Inner conductor (AES/EBU, DMX) [mm²]	: 0,14

Inner conductor Ø (power) [mm]	: 1,38

AWG (power)	: 15

AWG (AES/EBU, DMX)	: 25

Shielding (audio)	: Copper spiral, tin-plated

Shielding (AES/EBU, DMX)	: Copper spiral, tin-plated

Shielding factor [%]	: 95

Copper strands (power)	: 28

Copper strands (AES/EBU, DMX)	: 36

Copper strand Ø (power) [mm]	: 0,25

Copper strand Ø (AES/EBU, DMX) [mm]	: 0,07

Conductor insulation material (AES/EBU, DMX) : PVC

Conductor insulation Ø [mm]	: 0,00

Conductor insulation Ø (power) [mm]	: 2,80

Conductor insulation Ø (AES/EBU, DMX) [mm] : 1,15

Weight per 1 m [g]	: 144

UV-resistant	: yes

Fire load per m [kWh]	: 0,54

Style variant	: round

Packing	: bulk stock

Temperature min. [°C]	: -20

Temperature max. [°C]	: 70

Width [mm]	: 9,5

Height [mm]	: 9,5

* MONOLITH 1 COMPACT 동급이상품